Babbits

##### Tin Babbit and Lead Babbit (Chippings 0,2 – 0,5mm)

| RMs | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Sb | Cu | Pb | Bi | As | Fe | Zn | Cd | Al |
| А2573х | 6,20 | 6,0 | 0,20 | rem. | 0,056 | 0,028 | [0,0039]* | [0,0025] | 0,045 | [0,0041] |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Sb | Cu | Pb | Bi | As | Fe | Zn |
| А2621х | rem. | 8,30 | [8,4] | 0,65 | 0,019 | [0,0035] | [0,49] | 0,007 |
| А2622х | rem. | 9,8 | 7,2 | 0,24 | 0,027 | 0,0098 | [0,42] | [0,006] |
| А2623х | rem. | 11,10 | 6,60 | 0,34 | 0,060 | 0,017 | [0,22] | [0,025] |
| А2624х | rem. | 12,30 | [5,6] | [0,72] | 0,071 | [0,059] | [0,48] | [0,035] |
| А2625х | rem. | 13,4 | 3,91 | 1,01 | 0,084 | 0,073 | [0,52] | [0,045] |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Sb | Cu | Pb | Bi | As | Fe |
| А2632х | 12,6 | 14,2 | 1,18 | rem. | 0,045 | 0,096 | 0,014 |

# Chromium bromide

##### Chromium bromide (Chippings 0,2 – 0,5mm)

| RM | Composition, % (by weight) |  |  |
| --- | --- | --- | --- |
|  | B | Cr | C |
| А2085х | 15,13 | 75,16 | 1,32 |

Bronzes

##### Tin bronzes (Chippings 0,2 – 0,5mm)

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | P | Zn | Ni | Cu | Fe | Pb | Sb | Bi | Al | Si | S |
| М1276х | 7,07 | 0,307 | (0,095)* | 0,213 | 92,34 | 0,0099 | 0,026 | 0,0028 | 0,0024 | 0,0032 | 0,0029 | [0,002] |
| М1286х | 8,31 | 0,279 | 0,040 | 0,193 | rem. | <0,005 | 0,018 | 0,0024 | (0,0018) | <0,001 | <0,001 |  |
| М1755х | 8,73 | 0,108 | 0,159 | 0,78 | 89,43 | 0,273 | 0,309 | [0,096] | 0,012 | [0,05] | 0,072 | 0,0023 |
| М1833х | 7,77 | 0,180 | 0,116 |  | 91,39 | 0,068 | 0,43 | 0,0070 | 0,0031 | <0,001 | 0,0020 | 0,0022 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | P | Zn | Ni | Cu | Fe | Pb | Sb | Bi | Al | Si | S | Mg |
| М1566х | 4,05 | 0,106 | 2,65 | 0,29 | 92,75 | 0,042 | 0,021 | 0,0027 | 0,0015 | 0,0024 | <0,001 |  |  |
| М1863х | 3,72 | 0,018 | 4,08 |  | 89,68 | 0,040 | 2,44 | 0,0353 | 0,0028 | <0,001 |  | [0,0045] | <0,001 |
| М2003х | 3,91 | 0,023 | 4,52 | 0,38 | 87,1 | 0,106 | 3,94 | (0,13) | 0,0043 | <0,001 |  | 0,0027 |  |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Zn | Pb | P | Ni | Cu | Al | Fe | Si | Sb | Bi | As | S |
| М253х | 10,13 | 6,76 | 0,51 | 0,058 | 1,04 | 81,10 | [0,010] | 0,372 | [0,029] | 0,0011 | [0,0032] |  |  |
| М1376х | 7,61 | [4,24] | 0,416 | 0,024 |  | 87,31 | [0,0025] | 0,177 | 0,0060 | 0,221 | (0,0059) | 0,018 | 0,0020 |
| М254х | 11,65 | 4,26 | [0,40] | (0,048) | 0,52 | 82,75 | [0,007] | 0,285 | [0,010] | 0,0010 | 0,0066 |  |  |
| М1216х | 9,67 | 2,45 | 0,49 | 0,069 | 0,215 | rem. | 0,0255 | 0,229 | 0,037 | 0,31 | 0,0148 |  |  |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Zn | Pb | P | Ni | Cu | Al | Fe | Si | Sb | Bi | Mn | Mg |
| М696х | 4,29 | 6,9 | [5,5] | 0,084 | 1,13 | 81,11 | 0,0195 | 0,315 | 0,0288 | 0,29 |  | 0,124 | [0,009] |
| М1206х | 4,48 | 6,95 | 5,65 | 0,057 | 1,17 | 80,91 | [0,045] | 0,235 | [0,005] | 0,34 | [0,030] | 0,068 | [0,038] |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Zn | Pb | P | Ni | Cu | Al | Fe | Si | Sb | Mn | Mg | As | S |
| М836х | 4,22 | 3,92 | [16,8] |  | [0,14] | [73,54] | [0,017] | 0,382 | 0,048 | 0,516 | 0,169 |  |  |  |
| М1883х | 4,23 | 4,49 | 15,16 | 0,054 |  | rem. | 0,021 | 0,21 | 0,038 | 0,43 | 0, 071 | 0,0100 | 0,019 | [0,002] |

Tin bronzes (Chippings 0,2 – 0,5mm)

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Zn | Pb | P | Ni | Cu | Al | Fe | Si | Sb | Mn | Mg | As |
| М816х | 3,19 | 7,96 | 4,47 | 0,105 | 1,01 | 82,42 | [0,005] | 0,391 | 0,0183 | 0,48 | [0,13] | [0,002] |  |
| М1763х | 2,89 | 12,58 | 4,18 | 0,072 | 1,71 | rem. | <0,001 | 0,290 | 0,0075 | 0,29 |  |  | 0,047 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Zn | Pb | P | Ni | Cu | Al | Fe | Si | Sb | S |
| М1843х | 4,52 | 5,49 | 5,48 | <0,001 | 1,23 | 82,76 | <0,001 | 0,28 | [0,005] | 0,19 | [0,004] |
| М1903х | 6,29 | 4,99 | 2,49 | 0,083 |  | 85,46 | [0,007] | 0,198 | [0,007] | 0,41 |  |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Zn | Pb | P | Ni | Cu | Al | Fe | Si | Sb | Bi |
| М876х | 8,24 | 0,406 | 9,01 | [0,18]* | 0,306 | 81,26 | [0,003] | 0,211 | [0,008] | 0,350 | [0,04] |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Zn | Pb | P | Cu | Al | Fe | Si | Sb | Bi | As | S |
| М1526х | [10,5] | 0,56 | 0,052 | 0,88 | 87,12 | 0,0068 | 0,31 | 0,0081 | 0,117 | 0,010 | [0,12] | 0,0021 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Zn | Pb | Ni | P | Al | Fe | Mn | Cu | Sb | Si |
| М846х | 3,86 | [8,5] | [5,04] | 1,18 | [0,092] | [0,015] | 0,312 | [0,12] | 80,39 | 0,39 | 0,021 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Zn | Pb | Ni | P | Al | Fe | Mn | Cu | Sb | Si | S | As | Mg | Bi |
| М1764х | 2,40 | 10,48 | 3,21 | 1,10 | [0,08] | <0,001 | 0,218 | 0,041 | 82,09 | 0,18 | <0,001 |  | 0,035 | <0,001 | 0,013 |
| М1873х | 3,97 | 7,64 | 4,28 | 1,44 | 0,063 | [0,01] | 0,38 | 0,050 | 81,85 | 0,51 | 0,0073 | 0,0042 | 0,065 | <0,001 | 0,010 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Zn | Pb | Ni | P | Al | Fe | Cu | Sb | Si |
| М996х | 12,3 | 0,254 | [0,70] | 0,70 | 0,229 |  | 0,079 | 85,21 | 0,76 |  |
| М1026х | 18,4 | 0,52 | 0,313 |  | 0,040 | [0,001] | 0,099 | 80,39 | 0,21 | [0,004] |

Tin bronzes (Chippings 0,2 – 0,5mm)

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Zn | Pb | Ni | Al | Fe | Cu | Sb | Si | S |
| М346х | 7,39 | 3,98 | 3,04 | 1,39 | [0,005] * | 0,26 | 83,55 | 0,19 | [0,018] |  |
| М1893х | 7,61 | 4,19 | 2,48 | 1,83 | 0,0015 | 0,254 | 83,22 | 0,21 | 0,0012 | 0,0041 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Zn | Pb | Ni | P | Al | Fe | Cu | Sb | Si | S |
| М986х | [11,9] | 0,041 | 0,110 | 3,02 | 0,0033 | 0,0019 | 0,0053 | 84,93 | 0,081 |  |  |
| М1773х | 8,03 | 2,49 | 0,15 | 4,21 | 0,017 | <0,001 | 0,064 | 84,96 |  | <0,001 | 0,0040 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Zn | Pb | Ni | P | Al | Fe | Cu | Sb | Si | S | As | Bi |
| М1336х | 1,26 | (0,78) | (8,23) | 0,68 | [2,0] | 0,0040 | 0,290 | 86,02 | 0,284 | [0,02] |  | [0,1] | [0,3] |
| М1752х | 11,84 | 0,50 | 0,92 | 2,29 | 0,317 | [0,02] | 0,109 | 83,09 | 0,28 | 0,40 | 0,0023 |  | 0,027 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Zn | Pb | Ni | P | Fe | Cu | Si |
| М1813х | 6,12 | 0,71 | 0,022 | 0,073 | 0,071 | 0,58 | 90,63 | 1,87 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Zn | Pb | Ni | P | Al | Fe | Mg | Cu | Sb | Si | S | Zr | Cd | Bi |
| М1782х | 9,45 | 1,37 | 4,41 | 3,22 | 0,57 | <0,001 | 0,248 |  | 80,55 | [0,16] | <0,005 | 0,0032 |  |  | 0,012 |
| М1783х | 10,09 | 0,87 | 5,18 | 2,30 | 0,297 | [0,0033] | 0,166 |  | 80,71 | [0,12] | 0,018 | 0,0029 |  |  | 0,017 |
| М1793х | 8,21 |  | 13,78 | 3,64 | 0,125 | 0,016 | 0,47 | [0,03] | rem. | 0,17 |  | [0,002] | 0,017 | 0,069 |  |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | P | Zn | Ni | Cu | Fe | Pb | Sb | Bi | Al | Si | S | Mg |
| А4522х (М666х) | 3,98 | 0,023 | 3,98 |  | 87,75 | 0,031 | 4,02 | 0,0056 |  |  |  |  |  |
| А5086х (М1853х) | 7,40 | 0,20 | 0,010 | 0,11 | 91,9 | 0,0039 | 0,31 | 0,0058 | 0,0043 | 0,0015 | 0,0034 | 0,0027 | <0,001 |

Tin bronzes (Chippings 0,2 – 0,5mm)

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Zn | Pb | Ni | Cu | Al | Fe | Si | Sb | Mn |
| А793х | 5,63 | 5,81 | 4,51 | 0,44 | 83,49 |  | 0,080 |  | 0,043 |  |
| А1376х | 4,22 | 3,93 |  | [0,14]* | 73,5 | [0,018] | 0,38 | 0,047 | 0,52 | 0,17 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Zn | Pb | Ni | P | Fe | Cu | Sb | Si | Mn |
| А893х | 9,14 | 0,58 | 10,45 | 0,51 | [0,025] | [0,12] | [79,8] | 0,29 |  |  |
| А2603х | 4,49 | 3,11 | 8,42 | 0,33 | 0,034 | 0,75 | 82,15 | 0,41 | 0,20 | 0,21 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Zn | Pb | Ni | P | Fe | Cu | Sb | Si | Mn |
| А772х | 7,59 | 1,38 | 12,49 | 1,07 |  | [0,012] | 77,46 |  | [0,034] | [0,011] |
| А4015х (М956х) | 9,25 | 0,49 | 2,51 | 3,22 | 0,055 | 0,22 | 83,63 | 0,30 | [0,01] |  |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Ni | Si | Sn | Zn | Pb | Fe | Sb | P | Bi | Al |
| А3341х | 76,7 | 0,071 | 0,0012 | 15,49 | 0,049 | 7,04 | 0,032 | 0,58 | 0,052 | 0,0080 | <0,001 |
| А3342х | 78,5 | 0,12 | 0,0029 | 14,86 | 0,11 | 5,59 | 0,13 | 0,32 | 0,085 | 0,012 | <0,001 |
| А3343х | 77,6 | 0,19 | 0,025 | 17,79 | 0,19 | 3,40 | 0,27 | 0,20 | 0,13 | 0,017 | [0,022] |
| А3344х | 76,2 | 0,32 | 0,050 | 18,24 | 0,32 | 3,35 | 0,51 | 0,11 | 0,24 | 0,032 | [0,037] |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Zn | Pb | Ni | P | Al | Fe | Cu | Sb | Si |
| А1366х | 8,98 | 0,32 | 0,393 | 1,00 | 0,29 | 0,0021 | 0,308 | 88,62 | 0,020 | 0,140 |
| А3991х (М867х) | [9,01] | [0,31] | 0,391 | 1,01 | [0,29] | [0,002] | 0,305 | 88,62 | 0,0205 | 0,142 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Zn | Pb | Ni | P | Al | Fe | Cu | Sb | As | Bi |
| А1033х | 1,00 | 0,15 | 8,98 | 0,50 | 2,13 | [0,011] | 0,028 | 86,76 | 0,28 | 0,059 | 0,028 |

Tin bronzes (Chippings 0,2 – 0,5mm)

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Zn | Pb | Ni | P | Al | Fe | Cu | Sb | Si | S | As | Bi |
| А4576х (М826х) | 7,10 | (3,40)* | 5,22 | 1,92 | 0,0145 |  | 0,186 | 82,27 | 0,094 | 0,0073 |  | 0,026 | 0,0061 |
| А5566х (М1676х) | 10,43 | 0,81 | 0,14 | 2,01 |  | [0,003] | 0,049 |  | 0,52 | 0,0052 | 0,0028 |  | 0,017 |

##### Tin-free bronzes (Chippings 0,2 – 0,5mm, 0,3 – 0,8mm)

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Al | Fe | Mn | Ni | Si | Cu | Sn | Pb | P | Zn | As | Sb |
| М1052х | 4,63 | 0,42 | 0,408 | 0,248 | 0,069 | 93,71 | 0,143 | 0,012 | 0,037 | 0,245 | 0,0055 | 0,0039 |
| М1054х | 7,11 | 0,212 | 0,210 | 0,51 | 0,119 | 91,13 | 0,057 | 0,036 | [0,003] | 0,497 | 0,022 | 0,0021 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Al | Fe | Mn | Ni | Si | Cu | Sn | Pb | P | Zn | Sb |
| М756х | 10,40 | 0,94 | 2,08 | 1,03 | 0,26 | 83,38 | 0,19 | [0,21] | 0,094 | 1,29 | 0,0012 |
| М757х | 9,40 | 0,51 | 1,73 | 0,55 | 0,15 | 86,51 | 0,10 | 0,097 | 0,043 | 0,92 | 0,0010 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Al | Fe | Mn | Ni | Si | Cu | Sn | Pb | P | Zn | Sb |
| М115х | 10,51 | 3,69 | 2,34 | 0,52 | 0,241 | 82,3 | [0,13] | 0,030 | 0,019 | 0,208 | 0,0021 |
| М1106х | 10,42 | 3,61 | 1,85 | 0,206 | 0,124 | 83,02 | 0,106 | 0,035 | (0,0096) | 0,50 | 0,0019 |
| М1266х | 9,67 | 3,82 | 0,54 | 0,56 | 0,110 | 83,76 | 0,103 | 0,014 | 0,028 | 1,48 | 0,0046 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Al | Fe | Mn | Ni | Si | Cu | Sn | Pb | P | Zn | S | Bi | As | Sb |
| М1516х | 9,73 | 4,64 | 0,81 | 4,62 | 0,085 | 79,42 | 0,14 | 0,030 | 0,0038 | 0,50 | [0,001] | 0,0023 | 0,0023 | 0,0017 |

Tin-free bronzes (Chippings 0,2 – 0,5mm, 0,3 – 0,8mm)

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Al | Be | Fe | Ni | Si | Ti | Cu | Sn | Pb | Zn |
| М186х | 0,110 | 2,30 | 0,152 | 0,40 | 0,097 | 0,126 | 96,57 | 0,081 | 0,0041 | 0,021 |
| М1033х | [0,15] | 1,606 | 0,23 | 0,260 | 0,141 | 0,21 | 97,37 |  | 0,0053 |  |
| М1034х | [0,13] | 2,00 | 0,100 | 0,40 | 0,316 | 0,192 | 96,75 |  | [0,009] |  |
| М1042х | 0,112 | 1,941 | 0,086 | 0,186 | 0,130 |  | 97,24 | 0,104 | 0,0045 | 0,049 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Al | Fe | Mn | Ni | Si | Cu | Sn | Pb | P | Zn | As | Sb |
| М66х |  | 0,460 | 1,409 | 0,201 | 3,71 | 93,16 | 0,270 | 0,030 | 0,071 | 0,53 |  | 0,0018 |
| М196х | [0,02] | 0,284 | 0,374 | 3,11 | 0,97 | 94,86 | 0,113 | [0,15] | 0,0091 | 0,201 | [0,01] | [0,0034] |
| М1116х | 0,010 | 0,088 | [0,22] | 2,53 | 0,72 | 96,03 | 0,071 | 0,122 | 0,0055 | 0,076 |  |  |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Al | Fe | Mn | Ni | Si | Cu | Sn | Pb | P | Zn | As | Sb |
| М106ах | 10,82 | 4,70 | 0,318 | 5,334 | 0,133 | 78,14 | 0,106 | 0,032 | 0,027 | 0,50 |  | 0,0025 |
| М1236х | 9,90 | 4,34 | 0,179 | (4,2)* | 0,101 | 80,82 | 0,120 | 0,0225 | 0,0125 | 0,28 | <0,001 | <0,001 |

Tin-free bronzes (Chippings 0,2 – 0,5mm)

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Ni | Si | Sn | Pb | Fe | Sb | Mn | Al |
| М1386х | 88,15 | 0,149 | 0,080 | 0,165 | 1,34 | [2,03] | 0,31 | 0,71 | 7,01 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Ni | Si | Sn | Zn | Pb | Fe | Ti | Al | Be |
| М187х | 96,42 | 0,39 | 0,094 | 0,076 | 0,021 | [0,004] | 0,140 | 0,126 | 0,097 | 2,63 |
| М1044х | 96,26 | 0,304 | 0,270 | 0,084 | 0,130 | 0,0061 | 0,077 |  | 0,0263 | 2,559 |

Tin-free bronzes (Chippings 0,2 – 0,5mm)

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Ni | Si | Sn | Zn | Cr | As | Pb | Fe | P | Co |
| М277х | [99,2] | [0,013] | 0,046 |  | 0,042 | 0,53 |  | 0,0084 | 0,081 | [0,016] |  |
| М796х | 95,97 | 2,38 | 0,61 | 0,031 | 0,068 | [0,42] | [0,008] | 0,0039 | 0,10 |  | 0,28 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Ni | Si | Sn | Zn | As | Pb | Fe | Sb | Bi | P | Mg | Mn | S |
| М1416х | rem. | 1,34 | 0,109 | 0,50 | 0,228 |  | 21,55 | 0,30 | 0,128 |  | 0,113 |  | 4,48 |  |
| М1624х | 99,16 |  | [0,003]* |  | (0,0041) | 0,0031 | 0,0017 | [0,002] | 0,0026 | (0,0020) | [0,0028] | 0,68 | 0,016 | [0,002] |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Ni | Si | Sn | Zn | Cr | Ti | Pb | Fe | P | Co | Zr |
| М533х | 98,90 | 0,32 | 0,094 | 0,0033 | 0,0087 | 0,20 | 0,031 | 0,014 | 0,074 | 0,0012 | 0,12 | [0,036] |
| М535х | 97,48 | 0,79 | 0,25 | [0,0042] | 0,020 | 0,52 | [0,027] | 0,024 | 0,12 | [0,001] | 0,46 | [0,088] |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Ni | Si | Sn | Zn | Pb | Fe | V | P | B | Mn | C | Al |
| М1446х | 73,20 | 2,25 | 0,255 | 0,050 | 1,10 | 0,053 | 3,04 | 0,010 | 0,077 | 0,0089 | 12,01 | 0,024 | 7,92 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Al | Fe | Mn | Ni | Si | Cu | Sn | Pb | P | Zn | As | Sb |
| А3541х (М95х) | 5,93 | 0,523 | 0,523 | 0,533 | [0,12] | 91,47 | 0,094 | 0,036 | 0,023 | 0,64 | [0,008] | 0,0034 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Ni | Si | Sn | Zn | Cr | Pb | Fe | Mn | Co |
| А763х | 75,74 | 1,18 | 0,011 | 0,041 |  |  | 18,88 | 0,14 | 3,70 |  |
| А4491х (М545х) | 96,20 | [0,30] | [0,97] | 0,051 | [0,083] | 0,64 | [0,24] | 0,10 |  | [1,16] |

Tin-free bronzes (Chippings 0,2 – 0,5mm)

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Ni | Si | Sn | Zn | Pb | Fe | Sb | As | P | Bi | Al |
| А2366х | rem. | 3,74 | 0,029 | 0,25 | 3,87 | 19,24 | 0,40 | 4,30 | 0,094 | 0,22 | 0,026 |  |
| А3321х | [69,8] | 4,7 | 0,010 | 0,12 | 2,35 | 17,1 | 0,30 | 4,50 | 0,035 | 0,10 | 0,0097 | 0,0069 |
| А3323х | [69,1] | 3,30 | 0,050 | 0,35 | 3,84 | 19,5 | 0,10 | 3,10 | 0,10 | 0,25 | 0,031 | 0,025 |
| А3324х | [66,5] | 2,53 | 0,070 | 0,48 | 5,09 | 22,1 | 0,072 | 2,37 | 0,16 | 0,34 | 0,057 | 0,043 |

Tin-free bronzes (Chippings  0,3 – 0,8mm)

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Al | Ni | Fe | Zn | Si | Mg | Sb | Bi | P |
| А6233х (М2043х) | 86,33 | 7,37 | 3,86 | 1,84 | 0,38 | 0,076 | 0,070 | 0,0040 | 0,0030 | 0,012 |
| А6114х (М2044х) | 86,18 | 7,32 | 3,02 | 2,51 | 0,62 | 0,12 | 0,042 | 0,0067 | 0,0020 | 0,021 |

Copper Base Alloys (Chippings 0,2 – 0,5mm)

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Ni | Si | Sn | Zn | Cr | Pb | Fe | Sb | Bi | P | Mg | S | Co | Zr | Ti | C |
| М534х | 98,33 | 0,58 | [0,15] * | 0,0039 | 0,015 | 0,33 | 0,019 | 0,096 |  |  | 0,0012 |  |  | 0,221 | 0,053 | 0,022 |  |
| М1505х | 99,49 | 0,0066 | 0,013 |  | 0,0126 | 0,38 | 0,0039 | 0,0411 | 0,0039 | 0,0045 | 0,0053 | <0,001 | 0,0034 |  |  |  | [0,009] |

CLAYS

Clays (Chippings 0,2 – 0,5mm)

| RM | Composition, % (by weight) |  |  |  |
| --- | --- | --- | --- | --- |
|  | SiO2 | Fe2O3 | Na2O | Al2O3 |
| А921х | 0,023 | 0,14 | 0,95 | rem. |
| А922х | 0,046 | 0,095 | 0,72 | rem. |
| А925х | 0,20 | 0,031 | 0,27 | rem. |

graphite

Graphite (Chippings 0,2 – 0,5mm)

| RM | Composition, % (by weight) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Ni | Mn | Ti | H | O | S |
| А1711х | 20,3 | 27,1 |  |  |  |  |
| А1721х |  |  | 13,8 |  |  |  |
| А1741х |  |  |  | 2,55 | 0,94 | 0,161 |

COBALT BASE ALLOYS

Cobalt Base Alloys (Chippings 0,2 – 0,5mm)

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Co | Al | Bi | Fe | Si | Mn | Cu | As | Ni | Sn | S | Sb | Pb | C | P | Zn |
| А4151х | rem. | 0,080 | 0,0013 | 0,50 | [0,5]* | 0,055 | 0,095 | <0,001 | 0,74 | 0,0058 | 0,0043 | 0,0030 | 0,0056 | 0,19 | 0,00054 | 0,0066 |
| А4152х | rem. | 0,050 | 0,00048 | 0,11 | 0,30 | 0,045 | 0,119 | <0,001 | 0,92 | 0,027 | 0,00094 | 0,007 | 0,012 | [0,03] | 0,00026 | 0,0048 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Co | Al | Bi | Fe | Si | Mn | Cu | As | Ni | Sn | S | Sb | Pb | C | P | Zn |
| А4153х | rem. | 0,0051 | 0,00035 | 1,71 | [0,04] | 0,0109 | 0,046 | <0,001 | 0,29 | <0,001 | 0,0032 | 0,00038 | 0,0031 | 0,24 | 0,00047 | 0,0042 |
| А4154х | rem. | 0,0054 | [0,0003] | 1,29 | [0,1] | 0,018 | [0,02] | <0,001 | 0,30 | <0,001 | 0,0027 | [0,001] | 0,0016 | [0,1] | 0,0018 | 0,0056 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Co | Al | Bi | Fe | Si | Mn | Cu | As | Ni | Sn | S | Sb | Pb | C | P | Zn |
| А4155х | rem. | [0,1] | [0,0003] | 0,90 | 0,103 | 0,033 | 0,041 | [0,001] | 0,51 | 0,0017 | 0,0062 | 0,0020 | 0,0014 | 0,24 | [0,0004] | 0,0099 |
| А4156х | rem. | 0,10 | 0,0015 | [0,1] | [0,2] | 0,083 | 0,151 | [0,001] | 0,80 | 0,015 | 0,00064 | 0,0078 | 0,0030 | [0,2] | 0,00019 | 0,0041 |

concentrateS

Concentrates (Chippings 0,2 – 0,5mm)

| RM | Composition, % (by weight) |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Zn | As | S | Fe | Cu |
| А1551х | 0,27 | 0,08 | 39,0 | [35,5]* | [0,25] |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Zn | Cd | Fe | SiO2 | Cu | As | Pb | S |
| А1561х | 43,4 | 0,125 | 9,3 | 2,1 | 2,8 | 0,12 | 0,35 | [31] |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Ni | CaO2 | SiO2 | MgO2 | AlO2 | Sb | Bi | Se | Te | F |
| А2371х | 25,33 | 0,0058 | 6,41 | 17,00 | 3,05 | 6,90 | 0,00075 | 0,0011 | 0,038 | 0,0005 | 0,045 |

| RM | Composition, % (by weight) |  |
| --- | --- | --- |
|  | Fe | V2O5 |
| А2373х | 50,18 | 0,93 |

| RM | Composition, % (by weight) |  |
| --- | --- | --- |
|  | Au | Ag |
| А3071х | 42,2 | 72,4 |

ADDITIONAL ALLOYS

Additional Alloys (Chippings 0,2 – 0,5mm)

| RM | Composition, % (by weight) |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Si | Ti | B | Fe | Al |
| А721х | 1,25 | 5,63 | 0,91 | 0,24 | rem. |

| RM | Composition, % (by weight) |  |  |  |
| --- | --- | --- | --- | --- |
|  | Pb | As | Sb | Cu |
| А731х | 87,99 | 7,88 | 3,66 | 0,027 |

| RM | Composition, % (by weight) |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Mn | Fe | P | Cu | Si |
| А746х | 29,86 | 0,46 | 0,017 | 68,93 | 0,27 |

| RM | Composition, % (by weight) |  |  |
| --- | --- | --- | --- |
|  | Cu | Ti | Al |
| А1824х | 55,68 | 0,98 | rem. |
| А1825х | 53,67 | 0,53 | rem. |

Copper Base

Copper Base Alloys (Chippings 0,2 – 0,5mm)

| CRM | Composition, % (by weight) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Zn | Pb | P | Cu | Sb | Cd |
| М1393х | 0,192 | 0,170 | 0,100 | 6,50 | 90,57 | 1,99 | 0,27 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Zn | Pb | Ni | P | Al | Fe | Mg | Sb | Ti | Cu | Cd |
| А115х |  |  |  |  | 5,6 |  |  |  | 2,7 |  | 91,59 |  |
| А803х | 0,104 | 0,11 | 0,21 | 0,101 | 7,19 | 0,15 | 0,059 |  | 1,283 |  | 89,89 | 0,090 |
| А2264х |  |  |  |  | <0,001 |  | <0,001 | <0,001 |  | 0,37 | 99,62 |  |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Pb | Ni | Fe | Sb | S | As | Cu | Au | Ag | Bi |
| А931х | 0,038 | 0,026 | 0,0048 | 0,030 |  | 0,037 | 99,78 |  |  | 0,0010 |
| А932х | 0,054 | 0,048 | 0,0029 | 0,052 |  | 0,020 | 99,64 |  |  | 0,0020 |
| А1541х |  | 0,049 |  | 0,045 | 0,12 | 0,029 | 99,47 | [64 г/т]* | [115 г/т] | 0,0007 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Zn | Pb | Ni | P | Al | Fe | Mg | Mn | C | Sb | Si | S | As | Cu | Ag | Cr | Cd | Bi |
| А4426х (М1656х) | 0,113 | 0,040 | 0,111 | 0,137 | [0,042] | 0,0120 | 0,146 | [0,009] | 0,020 | [0,005] | (0,107) | 0,0191 | 0,0027 | 0,059 | rem. | 0,0075 | 0,071 | 0,062 | 0,060 |
| А4427х (М1657х) | 0,30 | 0,063 | 0,56 | 1,08 | 0,078 | 0,155 | 0,235 | [0,032] | 0,052 | [0,005] | (0,161) | 0,106 | [0,0027] | 0,27 | rem. | 0,0024 | 0,103 | 0,026 | 0,0080 |

Copper- phosphorous Base Alloys (Chippings 0,2 – 0,5mm, 0,3 – 0,8mm)

| RM | Composition, % (by weight) |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Cu | P | Fe | Ni | Sb |
| А3221х | 90,72 | 8,71 | 0,0070 | 0,0062 | <0,001 |
| А3222х | 88,60 | 11,00 | 0,0153 | 0,0058 | <0,001 |

Copper Base Alloys (Chippings 0,2 – 0,5mm, 0,3 – 0,8mm)

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Ag | Bi | Sb | As | Fe | Ni | Pb | Sn | S | C | Te | Cr | Zn | P | Si | Mg | Ce | Cd | Mn | Al | Au |
| А4002х (М1472х) | 99,98 | 0,00078 | 0,00036 | 0,00060 | 0,00039 | 0,00025 | 0,0021 | 0,0041 | 0,00058 | [0,0006] | [0,007]* | [0,0003] | 0,0019 | 0,00064 | 0,00022 | 0,00096 | 0,00023 | 0,00022 | 0,00051 | 0,00031 | 0,00055 |  |
| А4006х (М1476х) | 99,92 | 0,00202 | 0,0021 | 0,0038 | 0,0019 | 0,00154 | 0,0072 | 0,0043 | 0,00055 | 0,0011 | [0,0045] | [0,0015] | 0,00059 | 0,00194 | 0,00028 | 0,00071 | 0,00044 | 0,00101 | [0,0024] | 0,00030 |  | 0,00014 |
| А4008х (М1478х) | 99,91 | 0,0071 | 0,0101 | 0,0099 | 0,0040 | 0,0035 | 0,0143 | 0,0122 | 0,0039 | 0,00068 | [0,005] | [0,005] | 0,00073 | 0,0069 | 0,0027 | 0,0016 | 0,0019 | 0,0054 | 0,0100 | 0,00058 | 0,0021 | 0,00045 |
| А40011х (М14711х) | 99,68 | 0,060 | 0,030 | 0,050 | 0,015 | 0,0031 | 0,051 | 0,045 | 0,040 | [0,0007] | [0,005] | [0,01] | 0,00071 | 0,030 | 0,0019 | 0,0022 | [0,0006] | 0,018 | 0,030 | 0,0014 | [0,003] | 0,0010 |

| RM | Composition, % (by weight) |  |
| --- | --- | --- |
|  | Cu | S |
| А2271х | 99,95 | 0,012 |
| А2272х | 99,94 | 0,0094 |
| А2273х | 99,95 | 0,0068 |
| А2274х | 99,96 | 0,0047 |
| А2275х | 99,94 | 0,021 |

NICKEL BASE

Nickel Base Alloys (Chippings 0,2 – 0,5mm, 0,3 – 0,8mm)

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Ni | Cu | S | Fe | Mg | Mn | Pb | C | P | Bi | As | Sb | Zn | Cd | Sn | Al |
| М446х | rem. | 0,158 | [0,0071] | 0,19 | [0,11]* | 0,066 | 0,0049 | 0,14 | 0,0060 | 0,0059 | [0,003] | 0,00014 | 0,051 | 0,00048 | 0,0034 | 0,074 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Ni | Cu | S | Fe | Si | Mg | Mn | Pb | C | P | Bi | As | Sb | Zn | Cd | Sn |
| М1636х | rem. | 0,133 | 0,0095 | 0,132 | 0,188 | 0,0836 | 0,104 | 0,0047 | [0,03] | [0,003] | 0,00219 | <0,001 | 0,0023 | 0,0092 | 0,00046 | 0,0028 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Ni | Cu | S | Fe | Si | Mg | Mn | Pb | C | P | Bi | As | Sb | Zn | Sn | Al | Co |
| М1498х | rem. | 0,104 | [0,005] | 0,064 | 0,140 | [0,001] | 0,056 | 0,0034 | [0,1] | 0,0027 | 0,0041 | 0,0018 | [0,005] | 0,0072 | 0,0022 | 0,022 | 0,037 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Al | Si | Mn | Ni | Fe | Mg | Cu | Pb | C | P | Sb | Co |
| М616х | 1,76 | 0,98 | 2,01 | rem. | 0,38 | [0,02] | 0,30 | 0,0032 | [0,12] | 0,0080 | 0,0019 | 0,82 |
| М626х |  | 0,42 | 5,88 | rem. | 0,488 | [0,080] | 0,222 | 0,0045 | [0,11] | 0,0118 | 0,0026 | [0,060] |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Ni | Cu | Fe | Si | Mn | Sb | Cr | Al | Co |
| А253х | rem. | 0,25 | 0,37 | 0,36 | 0,32 | 0,0023 | 9,31 | 0,14 | 1,06 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Al | Si | Mn | Cr | Ni | Fe | Mg | Cu | Pb | S | Ti | C | P | Bi | As | Sb | Zr | Co |
| М1156х | 0,063 | 0,51 | 0,273 | [9,16] | rem. | 0,353 | (0,071) | 0,239 | 0,0034 | [0,0023] | (0,044) | 0,221 | 0,0020 | 0,0029 | 0,0012 | 0,0032 | 0,033 | (0,95) |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Fe | Mn | Zn | Ni | Cu | Si | Mg | Pb | P | Bi | As | Sb |
| М406х | 1,10 | 0,259 | [0,51] | [20,8] | 76,86 | 0,270 | [0,027] | [0,0052] | 0,015 | [0,0034] |  | 0,0079 |
| М416х | 0,092 | 0,142 | 0,304 | 16,36 | 83,13 | [0,0029] | [0,024] | 0,0034 | 0,0043 | 0,0033 | [0,0034] | 0,0031 |

##### Nickel Base Alloys (Chippings 0,2 – 0,5mm, 0,3 – 0,8mm)

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Fe | Zn | Ni | Cu | Si | Pb | S | C | P | Bi | As | Sb |
| М1013х | 0,0045 | rem. | 0,48 | 99,42 | <0,001 | 0,0080 | 0,0035 | 0,0097 | <0,001 | 0,0040 | 0,0095 | 0,0037 |
| М2013х | 0,141 | rem. | [4,6]* | 94,92 |  | 0,056 | 0,0059 | 0,0066 | [0,001] | 0,0053 |  | 0,0105 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Al | Fe | Mn | Zn | Ni | Cu | Pb |
| М367х | 1,79 | 0,58 | 0,088 | rem. | 7,30 | 90,13 | [0,001] |
| М368х | 2,48 | [0,93] | 0,335 | rem. | 13,04 | 83,08 | [0,004] |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Fe | Mn | Zn | Ni | Cu | Si | Mg | Pb | P | Bi | As |
| М386х | 0,393 | 0,0215 | 20,85 | 15,43 | 63,10 | [0,006] | [0,0004] | [0,023] | 0,0058 | 0,0020 | [0,01] |
| М596х |  |  | rem. | 15,88 | 53,88 |  |  | 1,78 |  |  |  |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Fe | Mn | Zn | Ni | Cu | Si | Pb | Al | C | P | Bi | As | Sb |
| М564х | 0,69 | [12,9] | rem. | 3,20 | 82,93 | 0,118 | 0,026 |  | [0,015] | 0,012 | 0,0050 | [0,010] | 0,0044 |
| М803х | 0,28 | 11,30 | rem. | 3,32 | 84,84 |  |  | 0,080 |  |  |  |  |  |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Fe | Mn | Zn | Ni | Cu | Si | Mg | Pb | S | C | P | Bi | As | Sb |
| М354х | 0,427 | 1,38 | 0,114 | 32,77 | 64,99 | 0,080 | 0,084 | 0,041 | [0,006] | [0,03] | 0,0102 | 0,0028 | 0,0029 | 0,0020 |
| М486х | 3,14 | 1,75 | rem. | 65,27 | 29,24 |  |  | 0,0081 | [0,01] | 0,290 | 0,0087 | [0,0056] | 0,014 | 0,0051 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Fe | Mn | Zn | Ni | Cu | Si | Pb | S | C | P | Bi | As | Sb | Sn | Ti |
| М524х | 1,33 | 0,71 | 0,89 | 6,63 | 90,15 | 0,269 | [0,0096] |  | [0,022] |  |  |  |  |  | [0,025] |
| М1923х | 0,89 | 0,33 | 0,73 | 5,62 | 91,74 | 0,156 | 0,156 | 0,0079 | [0,0046] | 0,012 | 0,0037 | [0,0005] | 0,011 | 0,14 |  |

##### Nickel Base Alloys (Chippings 0,2 – 0,5mm, 0,3 – 0,8mm)

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Si | Mn | Fe | Mg | Cu | Pb | C | P | Sb | Co |
| А4352х (М627х) | 0,61 | 4,02 | 1,03 | 0,104 | 0,67 | 0,0031 | [0,28]* | 0,023 | 0,0014 | [0,055] |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Al | Fe | Mn | Ni + Co | Cu | Mg | C | Zr |
| А2262х | 0,30 | 11,42 | 0,74 | 87,2 |  |  |  | 0,023 |
| А2265х |  | 0,040 | 0,41 | 82,99 | 16,95 | <0,001 | 0,0050 |  |

Nickel-Copper Base Alloys (Chippings 0,2 – 0,5mm, 0,3 – 0,8mm)

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Al | Fe | Mn | Zn | Ni | Cu | Si | Pb | S | C | P | Sn | Cr |
| М886х | 0,0081 | 0,482 | 0,40 | 0,307 | [11,79] | 87,03 | [0,0079] | 0,028 | 0,0029 | 0,0101 | 0,0074 | 0,024 | [0,006] |
| М887х | [0,12] | 1,04 | 0,311 | 0,50 | (14,20) | 83,08 | 0,170 | 0,046 | 0,0028 | [0,11] | 0,0101 | (0,100) | 0,289 |

| CRM | Composition, % (by weight) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Fe | Ni | Cu | Si | Ti | Zr |
| М763х | 0,082 | 18,97 | 80,29 | 0,103 | 0,27 | 0,125 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Fe | Mn | Ni | Cu | Si | Mg | Pb | S | C | P | Bi | As | Sb | РЗМ |
| М1176х | (2,08) | (5,13) | rem. | 2,65 | 0,23 | [0,05] | 0,0030 | [0,003] | 0,024 | 0,022 | 0,00061 | 0,035 | 0,0025 | 0,29 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Fe | Mn | Ni +Co | Cu | Si | Mg | Pb | S | C | P | Bi | As | Sb |
| А2266х | 0,100 | 1,71 | 40,14 | 58,07 | 0,020 | 0,055 | 0,0015 | 0,0063 | 0,083 | 0,0018 | 0,0019 | 0,0094 | 0,00203 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Fe | Mn | Ni | Cu | Si | Mg | Pb | P | Bi | Sb |
| А3161х (М292х) | 0,430 | 1,36 | [40,1] | 57,10 | 0,197 | 0,078 | [0,0013] | 0,0062 | 0,0031 | 0,0027 |
| А3162х (М294х) | 0,28 | 0,407 | [44,7] | 53,81 | 0,14 | 0,054 | 0,0016 | 0,0037 | 0,0020 | 0,0011 |

Nickel-Copper Base Alloys (Chippings 0,2 – 0,5mm, 0,3 – 0,8mm)

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Zn | Ni | Cu | Si | Mg | S | C | As | Sb | Co |
| А3014х | 20,2 | 13,8 | 65,2 | 0,15 | 0,051 | 0,0018 | 0,0071 | 0,011 | 0,0023 | 0,12 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Fe | Mn | Zn | Ni | Cu | Si | Pb | P | Bi | As | Sb | Co | Sn |
| А3545х (М55х) | 0,98 | 1,06 | 0,112 | 31,0 | 66,5 | 0,122 | 0,0051 | 0,0106 | 0,0028 | [0,0025] | 0,0021 | 0,036 |  |
| А4541х (М137х) | 1,83 | 1,00 | [0,78] | [6,8] | 89,32 | 0,161 | 0,010 | [0,075] | 0,0029 | [0,06] * | 0,0041 |  | 0,21 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Al | Mn | Ni | Cu | Si | B | Zr |
| А2261х | 1,47 | 1,64 | rem. | 56,02 | 0,24 | 0,010 | 0,058 |
| А2263х |  | 3,74 | 5,23 | 91,1 |  |  |  |

SOLDERS

Solders (Chippings 0,2 – 0,5mm)

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Zn | Pb | Ni | P | Fe | Cu | Sb | Si | S | Zr | Bi |
| М1323х |  | 25,55 | 0,031 | 0,122 | 5,28 | [0,50]* | 68,25 | 0,0033 |  | 0,0014 |  | [0,0019] |
| М1453х | 3,72 | 0,011 | 0,012 |  | 5,73 | 0,118 | 89,94 | 0,029 | 0,087 |  | 0,013 | 0,0030 |

Solders (Chippings 0,2 – 0,5mm, 0,3 – 0,8mm)

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Sb | Cd | Cu | Pb | Bi | As | Fe | Ni | S | Zn | Al |
| А3481х | 63,34 | 0,051 | 0,0029 | 0,046 | rem. | 0,096 | 0,029 | 0,029 | 0,030 | 0,0013 | 0,0071 | 0,0023 |

ALUMINIUM BASE

Al/Si/Mg (Chippings 0,2 – 0,5mm)

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Mg | Si | Mn | Cu | Ti | Ni | Fe | Zn | Pb | Sn | As | Be | Zr |
| М1346х | 0,473 | 10,53 | 0,46 | 1,081 | 0,15 | 0,34 | 1,23 | 0,60 | 0,032 | 0,013 |  |  |  |
| М1353х | [0,29]* | 10,59 | 0,44 | 0,97 | 0,13 | 0,137 | 0,95 | 0,29 | 0,100 | 0,041 |  | [0,023] | 0,12 |
| М1803х | [0,30] | 6,46 | 0,48 | 0,283 | 0,13 |  | 1,09 | 0,31 | 0,069 | 0,0094 | 0,0028 | [0,02] | <0,02 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Mg | Si | Mn | Cu | Fe | Zn | Pb | Sn | As | Be | Cd | Sb |
| М1463х | 1,00 | 5,93 | 0,55 | 1,29 | 1,02 | 0,29 | 0,089 | 0,011 | <0,0002 | 0,0011 | 0,054 | 0,0057 |
| М1464х | 0,60 | 6,81 | 0,69 | 1,01 | 1,13 | [0,2] | 0,11 | 0,0053 | <0,0002 | 0,0015 | 0,035 | 0,0100 |
| М1465х | 0,25 | 7,56 | 0,135 | 0,52 | 0,32 | 0,102 | 0,20 | [0,003] | <0,0002 | 0,0037 | 0,0100 | 0,0115 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Mg | Si | Mn | Cu | Ti | Fe | Zn | Pb | Sn | Zr | Ca | Na | Al |
| А2021х | 0,16 | 6,15 | 0,73 | 0,17 | 0,039 | 1,26 | 0,083 | 0,020 | 0,0076 | 0,30 | 0,18 | 0,0051 | rem. |
| А3863х | 0,075 | 12,39 | 0,50 | 0,84 | 0,103 | 1,81 | 0,29 |  |  | 0,060 |  |  | rem. |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Mg | Si | Mn | Cu | Ni | Fe | Zn | Pb | As | Be | Al |
| А3156х | 0,39 | 6,99 | 0,48 | 1,77 | 0,46 | 1,09 | 0,69 | 0,17 | 0,014 | 0,042 | rem. |
| А4521х (М1253х) | 0,455 | 6,29 | 0,45 | 1,73 | 0,67 | 1,56 | 0,44 |  |  |  | rem. |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Si | Fe | Cu | Mn | Mg | Cr | Zn | Ti | Zr |
| А4653х (М2173х) | 0,89 | 0,68 | 0,36 | 0,35 | 0,90 | 0,21 | 0.31 | 0,15 | 0,045 |

Al/Si/Cu (Chippings 0,2 – 0,5mm)

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Mg | Si | Mn | Cu | Ni | Fe | Zn | Pb | Sn | As | Be | Cd | Sb |
| М1461х | [0,4] | 3,94 | 0,148 | 2,41 |  | 0,52 | 0,081 | 0,034 | 0,041 | <0,0002 | 0,00084 | 0,0092 | 0,053 |
| М1462х | 0,75 | 4,86 | 0,250 | 2,37 |  | 0,65 | 0,068 | 0,038 | 0,025 | <0,0002 | 0,0011 | 0,025 | 0,018 |
| М1963х | [0,51] | 5,33 | 0,30 | 8,80 | 0,41 | 0,99 | 0,51 | 0,35 | 0,14 |  |  |  | 0,23 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Mg | Si | Mn | Cu | Ti | Ni | Fe | Zn | Pb | Sn | As | Be | Zr |
| М1823х | 0,475 | 4,53 | 0,40 | 1,21 | 0,10 | 0,136 | 1,09 | 0,381 | 0,079 | 0,011 | 0,0027 | [0,022] * | 0,011 |
| М2073х | [0,44] | 5,57 | 0,32 | 2,85 | 0,15 | 0,342 | 0,76 | 1,21 | 0,23 |  | [0,004] | [0,0005] |  |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Mg | Si | Mn | Cu | Ti | Ni | Fe | Zn |
| М2033х | [0,3] | 4,33 | 0,393 | 3,87 | 0,228 | 0,67 | 1,21 | 1,46 |
| М2083х | [0,24] | 4,22 | 0,253 | 2,85 | 0,23 | 0,077 | 0,77 | 0,121 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Mg | Si | Mn | Cu | Ni | Fe | Zn | Pb | Sn | As | Sb | Al |
| А644х | 0,66 | 6,41 | 0,51 | 8,66 | 0,82 | 1,51 | 0,19 | 0,11 | 0,30 |  | 0,070 | rem. |
| А1026х | 0,89 | 6,02 | 0,45 | 7,25 | 0,28 | 1,13 | 1,04 | 0,25 | 0,051 |  |  | rem. |
| А1254х | 0,66 | 3,80 | 0,72 | 3,47 | 0,23 | 1,18 | 0,38 | 0,10 |  | 0,0068 |  | rem. |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Mg | Si | Mn | Cu | Ti | Ni | Fe | Zn | Pb | Sn | Ca | Cr | Al |
| А2042х | 2,05 | 10,0 | 0,101 | 0,79 | 0,27 | 0,70 | 0,82 | 0,21 | 0,025 | 0,045 | 0,11 | 0,19 | rem. |
| А3574х | 0,23 | 12,4 | 0,20 | 0,60 | 0,066 | 1,33 | 0,73 | 0,22 | 0,080 |  |  | 0,13 | rem. |
| А3575х | 1,08 | 9,92 | 0,48 | 2,50 | 0,13 | 0,48 | 1,26 | 0,51 | 0,031 |  |  | 0,24 | rem. |

Al/Cu (Chippings 0,2 – 0,5mm)

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Mg | Si | Mn | Cu | Ti | Ni | Fe | Zn | Zr | Cd |
| М2056х | [0,0022]* | [0,27] | 0,39 | 5,00 | 0,356 |  | 0,24 | 0,238 | 0,060 | 0,239 |
| М2063х | 0,067 | 0,38 | 0,76 | 5,09 | 0,297 | 0,112 | 0,37 | 0,191 | 0,11 |  |

Al/Mg (Chippings 0,2 – 0,5mm)

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Mg | Si | Mn | Cu | Ti | Fe | Zn | Be | Zr |
| М1972х | 4,91 | 0,23 | 1,03 | 0,33 | 0,111 | 0,82 |  |  | 0,043 |
| М1983х | 10,75 | 0,14 | 0,089 | 0,095 | [0,1] | 0,175 | 0,091 | 0,034 | 0,063 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Si | Fe | Cu | Mn | Mg | Cr | Zn | Ti | Pb | As | Be |
| М1912х | 1,01 | 0,94 | [0,18] | 0,78 | 4,14 | 0,192 | 0,48 | 0,13 | 0,031 | [0,001] | 0,0034 |
| М1913х | 0,67 | 0,66 | 0,41 | 0,55 | 5,02 | 0,129 | 0,62 | 0,046 | 0,051 | 0,00204 | 0,002 |
| М1914х | 0,44 | 0,44 | 0,258 | 0,35 | 5,79 | 0,055 | 0,69 | 0,035 | 0,076 | [0,009] | 0,00093 |
| М1915х | [0,14] | 0,20 | 0,065 | [0,19] | 6,54 | 0,055 | 0,188 | [0,004] | 0,17 | [0,003] | [0,0005] |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Si | Fe | Cu | Mn | Mg | Cr | Zn | Ti | Pb | As | Be |
| М1943х | 1,85 | 0,57 | 0,770 | 0,50 | 1,56 | 0,030 | 0,47 | 0,131 | 0,080 | <0,001 | 0,0010 |
| М1944х | 0,89 | 0,45 | 0,168 | 0,198 | 1,93 | 0,23 | 0,50 | 0,083 | 0,060 | [0,005] | 0,0016 |
| М1945х | 1,04 | 0,215 | 0,405 | 0,099 | 2,93 | [0,09] | 0,120 | 0,067 | 0,031 | <0,002 | 0,0033 |
| М1946х | 0,21 | 0,117 | 0,082 | 0,080 | 3,87 | 0,28 | [0,15] | 0,048 | 0,158 | <0,001 | 0,0064 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Mg | Si | Mn | Cu | Ti | Fe | Zn | Be | Zr | Al |
| А1533х | 8,61 | 0,16 | 0,044 | 0,35 | 0,076 | 0,21 | 0,20 | 0,014 | 0,22 | rem. |

Al/Cu/Mg; Al/Cu/Mn (Chippings 0,2 – 0,5mm)

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Si | Fe | Cu | Mn | Mg | Cr | Zn | Ti | Ni | Zr |
| А4533х (М2183х) | 0,76 | 0,71 | 4,03 | 0,52 | 1,55 | 0,060 | 0,25 | 0,15 | 0,11 | 0,023 |
| А4553х (М2203х) | 0,45 | 0,45 | 2,59 | 0,30 | 0,36 | 0,030 | 0,15 | 0,112 |  | 0,012 |
| А4953х (М2243) | 0,71 | 1,41 | 1,91 | 0,074 | 1,39 | 0,026 | 0,26 | 0,042 | 0,94 |  |

Al/Mn (Chippings 0,2 – 0,5mm)

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Si | Fe | Cu | Mn | Mg | Cr | Zn | Ti | Ni | Zr | Be |
| А4433х (М2163х) | 1,07 | 0,42 | 0,077 | 0,92 | 0,13 | 0,014 | 0,057 | 0,065 | 0,021 | 0,012 | 0,00049 |

Al/Zn/Mg (Chippings 0,2 – 0,5mm)

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Si | Fe | Cu | Mn | Mg | Cr | Zn | Ni | Zr | Be |
| А5087х (М1933х) | 0,28 | 0,84 | 1,78 | 0,41 | 1,57 | 0,091 | 5,3 | 0,11 | 0,060 | 0,0014 |

Silumins (Chippings 0,2 – 0,5mm)

| CRM | Composition, % (by weight) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Si | Mn | Cu | Ti | Fe | Zn | Ca |
| М1952х | 11,23 | 0,253 | 0,120 | 0,21 | 0,94 | 0,30 | [0,04] |
| М1953х | 12,60 | 0,124 | 0,051 | 0,131 | 0,45 | 0,182 | [0,03] |
| М1954х | 13,05 | 0,061 | 0,017 | 0,089 | 0,35 | 0,079 | [0,01] |

Various Aluminium Alloys (Chippings 0,2 – 0,5mm)

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Si | Fe | Cu | Mn | Mg | Zn | Ti | As | Be |
| М2116х | 0,29 | 0,48 | 0,119 | 0,111 | 0,067 | 0,052 | 0,064 | 0,017 | 0,0098 |
| М2117х | 0,69 | 0,74 | 0,23 | 0,212 | 0,127 | 0,146 | 0,23 | 0,025 | 0,014 |

Various Aluminium Alloys (Chippings 0,2 – 0,5mm)

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Fe | Si | Cu | Zn | Ti | Mn | Mg | As | Be |
| М2111х | 0,070 | 0,101 | 0,012 | 0,018 | 0,0036 | 0,0123 | 0,017 | [0,0002]* | 0,0014 |
| М2112х | 0,082 | 0,114 | 0,015 | 0,023 | 0,0083 | 0,021 | 0,015 | [0,0004] | 0,0024 |
| М2113х | 0,121 | 0,17 | 0,146 | 0,053 | 0,020 | 0,053 | 0,021 | 0,0026 | 0,0026 |
| М2114х | 0,234 | 0,18 | 0,118 | 0,046 | 0,028 | 0,058 | 0,029 | 0,0047 | 0,0042 |
| М2115х | 0,269 | 0,18 | 0,075 | 0,036 | 0,056 | 0,075 | 0,043 | 0,010 | 0,0079 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Mg | Si | Mn | Cu | Ti | Fe | Zn | Be | Zr | Al |
| А3102х | 2,10 | 0,68 | 0,41 | 0,101 | 0,39 | 0,43 | 4,68 | 0,065 | 0,056 | rem. |

| RM | Composition, % (by weight) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Mg | Cu | Zn | Si | Pb | Sn | Al |
| А1905х | 0,157 | 0,150 | 0,100 | 0,98 | 0,100 | 0,094 | rem. |
| А1916х | 3,03 | 2,98 | 0,79 | 1,21 | 0,20 | 0,093 | rem. |
| А1917х | 3,00 | 2,96 | 0,83 | 2,64 | 0,29 | 0,20 | rem. |
| А1918х | 3,02 | 3,45 | 3,04 | 3,80 | 0,30 | 0,19 | rem. |
| А1919х | 2,80 | 3,95 | 3,26 | 4,95 | 0,29 | 0,21 | rem. |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Sb | Cu | Si | Ti | Al | Fe | Zn | Pb |
| А131х | 17,1 | 0,047 | 1,81 | 0,58 | 0,015 | rem. | 0,27 | 0,13 | 0,031 |
| А132х | 18,4 | 0,082 | 1,21 | 0,51 | 0,031 | rem. | 0,33 | 0,16 | 0,047 |
| А133х | 21,4 | 0,10 | 0,85 | 0,30 | [0,073] | rem. | [0,75] | 0,21 | 0,10 |
| А134х | [22,9] | 0,13 | 0,50 | 0,18 | 0,087 | rem. | 0,28 | 0,27 | 0,10 |
| А135х | 24,1 | [0,19] | 0,28 | 0,12 | 0,24 | rem. | 1,08 | 0,32 | 0,18 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Mg | Mn | Sb | Cu | Si | Ti | Al | Fe | Zn |
| А4135х | 3,89 | 0,10 | 1,03 | 0,0073 | 6,76 | 0,20 | 0,030 | rem. | 0,63 | 0,042 |

Various Aluminium Alloys (Chippings 0,2 – 0,5mm)

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sb | Mn | Mg | Cu | Si | Te | Ti | Fe | Zn | Pb | Sn | Al |
| А703х | 4,96 | 0,10 | [0,047]* | 0,9 | 0,20 | [0,11] | 0,078 | 0,26 | 0,19 | 0,200 | 0,074 | rem. |
| А2583х | 1,64 | 0,104 | 0,33 | 1,04 | 9,46 | 0,020 | 0,14 | 0,50 | 0,13 | 0,060 | 0,107 | rem. |

| RM | Composition, % (by weight) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Mn | Mg | Cu | Si | Fe | Zn | Al |
| А1682х | 0,45 | 0,47 | 2,56 | 0,76 | 0,66 | 0,88 | rem. |
| А1684х | 0,13 | 0,22 | 4,50 | 0,42 | 0,20 | 0,32 | rem. |
| А1685х | 0,062 | 0,10 | 5,77 | 0,25 | 0,085 | 0,12 | rem. |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Mn | Mg | Cu | Ni | Si | Ti | Fe | Zn | Pb | Cr | Al |
| А1016х | 0,88 | 1,48 | 1,97 | 2,75 | 17,3 | 0,15 | [0,49] | 0,103 | 0,075 | [0,049] | rem. |
| А2406х | 0,50 | 0,97 | 3,17 | 1,63 | 10,71 |  | 0,97 |  |  |  | rem. |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Mn | Mg | Cu | Si | Ti | Fe | Zn | Pb | Al | Zr | B | Cd |
| А1234х | 0,12 | 0,34 | 4,00 | 8,01 | 0,30 | 0,86 |  |  | rem. |  |  |  |
| А2283х | 0,29 | [0,066] | 3,27 | 7,71 | [0,25] | 0,39 | 0,22 | 0,19 | rem. | [0,1] | [0,08] | 0,14 |
| А1866х | 0,49 | 0,0083 | 4,87 |  | 0,24 | 0,31 | 0,101 | 0,29 | rem. | 0,11 |  | 0,13 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Mg | Si | Ti | Fe | Zn | Al | Zr | Be |
| А2011х | 9,7 | 1,56 | 0,022 | 0,36 | 0,030 | rem. | 0,034 | 0,11 |
| А2012х | 10,6 | 1,22 | 0,033 | 0,51 | 0,050 | rem. | 0,041 | 0,046 |
| А2013х | 12,4 | 1,02 | 0,046 | 0,72 | 0,068 | rem. | 0,018 | 0,053 |
| А2014х | 13,33 | 0,71 | 0,068 | 1,09 | 0,102 | rem. | 0,058 | 0,032 |
| А2015х | 14,9 | 0,56 | 0,14 | 1,71 | 0,20 | rem. | 0,13 | 0,019 |

Various Aluminium Alloys (Chippings 0,2 – 0,5mm)

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Mn | Mg | Cu | Si | Ti | Fe | Zn | Pb | Sn | Al | Zr | Ca | Na |
| А2022х | 0,105 | 0,20 | 0,18 | 6,84 | 0,042 | 1,10 | 0,13 | 0,028 | 0,0050 | rem. | 0,17 | 0,039 | [0,0027]* |
| А2025х | 0,14 | 0,38 | 0,39 | 9,0 | 0,094 | 0,28 | 0,36 | 0,053 | 0,017 | rem. | 0,051 | 0,0075 | <0,002 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Mn | Mg | Cu | Si | Ti | Fe | Zn | Al | Zr | Be |
| А1992х | 0,046 | 9,32 | 0,35 | 0,30 | 0,019 | 0,136 | 0,057 | rem. | 0,032 | 0,047 |
| А1994х | 0,11 | 10,32 | 0,67 | 0,17 | 0,11 | 0,87 | 0,13 | rem. | 0,21 | 0,0012 |
| А1995х | 0,28 | 10,15 | 0,052 | 0,086 | 0,040 | 0,31 | 0,097 | rem. | 0,32 | 0,022 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Mn | Mg | Cu | Si | Ti | Fe | Zn | Pb | Sn | Al | Zr | Be | B |
| А1876х | 0,12 | 0,049 | 0,139 | 7,73 | 0,16 | 0,31 | 0,26 | 0,028 | 0,0069 | rem. | 0,078 | [0,10] |  |
| А2933х | 0,28 | 0,32 | 0,42 | 6,81 | 0,12 | 0,88 | 0,22 | 0,048 | 0,015 | rem. | 0,047 | 0,14 | [0,008] |
| А2935х | 0,44 | 0,93 | 0,25 | 4,69 | 0,16 | 2,10 | 0,31 | 0,070 | 0,016 | rem. | 0,039 | 0,27 | 0,0073 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Mn | Mg | Cu | Si | Ti | Fe | Zn | Ni | Al |
| А1696х | 0,51 | 0,26 | 0,61 | 6,54 |  | 1,17 | 10,50 | [0,26] | rem. |
| А1063х | 0,15 | 5,99 | 0,22 | 0,28 | 0,10 | 0,40 |  |  | rem. |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Mn | Mg | Cu | Ni | Si | Ti | Fe | Zn | Pb | Sn | Cr | Al | Ca |
| А2041х | 0,078 | 1,43 | 0,52 | 0,50 | 8,96 | 0,45 | 1,11 | 0,39 | 0,0059 | 0,024 | 0,34 | rem. | 0,041 |
| А2044х | 0,21 | 0,54 | 1,56 | 1,03 | 11,6 | 0,095 | 0,43 | 0,078 | 0,019 | 0,0063 | 0,081 | rem. | 0,048 |
| А2045х | 0,42 | 0,36 | [2,4] | 1,99 | 13,0 | 0,070 | 0,34 | 0,070 | 0,032 | 0,0038 | 0,071 | rem. | 0,069 |

| CM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Mn | Mg | Cu | Si | Ti | Fe | Zn | Pb | Sn | Al |
| А1673х | 0,18 | 0,49 | 6,06 | 0,84 | 0,102 | 0,79 | 0,10 | 0,69 | 0,99 | rem. |

Various Aluminium Alloys (Chippings 0,2 – 0,5mm)

| CM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sb | Mn | Mg | Cu | Ni | Si | Ti | Fe | Zn | Pb | Sn | Al | P |
| А1893х | 0,067 | 0,12 | 0,54 | 1,37 | 1,08 | 13,86 |  | 1,06 | 0,099 | 0,050 | 0,0092 | rem. | 0,0046 |

| CM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Mn | Mg | Cu | Ni | Si | Ti | Fe | Zn | Pb | Sn | Al |
| А2032х | 0,22 | 0,21 | 2,56 | 0,125 | 10,6 | 0,078 | 0,39 | 0,28 | 0,021 | 0,098 | rem. |
| А2035х | 0,76 | 0,048 | 1,50 | 0,60 | 12,37 | 0,42 | 1,21 | 0,94 | 0,072 | 0,030 | rem. |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Mn | Mg | Cu | Si | Ti | Fe | Zn | Al | Be | K | Na |
| А2051х | 1,10 | 4,15 | 0,69 | 1,27 | 0,049 | 0,090 | 0,062 | rem. | 0,0026 | [0,03]* | [0,09] |
| А2052х | 0,94 | 4,57 | 0,90 | 1,58 | 0,084 | 0,24 | 0,087 | rem. | 0,0039 | [0,03] | [0,06] |
| А2054х | 0,53 | 5,47 | 1,14 | 1,97 | 0,13 | 0,47 | 0,14 | rem. | 0,0087 | [0,07] | [0,03] |
| А2055х | 1,20 | 6,80 | 1,32 | 2,30 | 0,35 | 0,58 | 0,24 | rem. | 0,0050 | [0,09] | [0,02] |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Mn | Mg | Cu | Ni | Si | Ti | Fe | Zn | Pb | Cr | Al | Ca | Na |
| А2415х | 0,155 | 0,39 | 1,30 |  | 1,18 |  | 0,63 | 4,97 | 1,16 |  | rem. |  |  |
| А2837х |  | 0,12 | 0,016 |  | 0,042 |  | 0,048 | 0,11 |  |  | rem. |  |  |
| А3745х | 0,33 | 0,248 | 3,16 | 0,018 | 9,78 | 0,36 | 0,75 | 0,71 |  | 0,26 | rem. | 0,0039 | 0,051 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Mn | Mg | Cu | Ni | Si | Fe | Zn | Sn | Al |
| А4091х | 0,022 | 0,28 | 1,86 | 0,73 | 2,75 | 0,26 | 0,034 | 1,60 | rem. |
| А4092х | 0,040 | 0,14 | 1,50 | 0,49 | 2,03 | 0,73 | 0,077 | 2,44 | rem. |
| А4093х | 0,050 | 0,12 | 0,85 | 0,30 | 1,65 | 0,55 | 0,096 | 3,54 | rem. |
| А4094х | 0,075 | 0,13 | 2,73 | 0,139 | 1,26 | 0,32 | 0,056 | 4,06 | rem. |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Mn | Mg | Cu | Ni | Si | Ti | Fe | Zn | Cr | Al | Zr |
| А4412х (М2192) | 0,67 | 2,05 | 4,00 | 0,14 | 0,37 | 0,029 | 0,31 | 0,50 | 0,009 | rem. | 0,013 |
| А4414х (М2194) | 0,35 | 1,11 | 4,93 | 0,048 | 1,02 | 0,10 | 0,70 | 0,10 | 0,08 | rem. | 0,024 |

COPPER BASE

Brass (Chippings 0,2 – 0,5mm, 0,3 – 0,8mm)

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Pb | Fe | Mn | Ni | P | Sb | Zn |  |
| М1136х | 63,03 | 0,083 | 0,090 | 0,094 | 0,078 | 0,0166 | 0,0058 | 36,46 |  |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Pb | Fe | Al | Sn | Si | Ni | Zn | Sb | Bi | P |
| М746х | 94,84 | 0,022 | 0,080 | 0,083 | 0,094 | 0,078 | 0,124 | 4,76 | 0,0035 | 0,0016 | 0,0093 |
| М379х | 89,28 | 0,032 | 0,096 |  |  |  |  | [10,55]* | 0,0054 | (0,0021) | 0,0057 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Pb | Fe | Sn | Si | Ni | Zn | Sb | Bi | P |
| М1743х | 83,92 | 0,058 | 0,043 | 0,010 | 0,0012 | 0,203 | 16,15 | 0,015 | 0,0080 | 0,0089 |
| М377х | 80,01 | [0,027] | 0,090 |  |  |  | 19,82 | 0,0053 | 0,0018 | 0,0043 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Pb | Fe | Sn | As | Zn | Sb | Bi | P |
| М205х | 69,95 | 0,043 | 0,056 | 0,0062 | 0,0208 | [29,8] |  | (0,0016) | [0,002] |
| М1226х | 70,70 | 0,0299 | 0,0661 | 0,00413 | 0,00150 | rem. | 0,0064 | 0,00238 | 0,00327 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Pb | Fe | Mn | Al | Si | Ni | Zn | Sb | Bi | P |
| М776х | 78,41 | 0,073 | 0,080 | 0,098 | 1,88 | 0,124 | 0,84 | 18,57 | 0,0046 | [0,0021] | 0,0033 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Pb | Fe | Mn | Al | Sn | Zn | Sb | Bi | P |
| М162х | 60,63 | 0,42 | 1,34 | 0,35 | 1,30 | 0,107 | [35,7] | 0,0080 | [0,005] | 0,0078 |
| М1182х | 61,19 | 0,43 | 1,01 | 0,221 | 1,93 | 0,102 | rem. | 0,0093 | [0,001] | [0,045] |

Brass (Chippings 0,2 – 0,5mm, 0,3 – 0,8mm)

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Pb | Fe | Mn | Al | Sn | Ni | Zn | Sb | Bi | P |
| М221х | 59,58 | 0,0082 | 0,203 | 1,21 | 3,96 | 0,39 | 2,40 | 32,4 | [0,0036] | [0,0025] | [0,0089] |
| М1296х | 58,43 | 0,119 | 0,53 |  | 3,29 |  | 2,79 | rem. | 0,0055 | 0,0031 | 0,012 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Pb | Fe | Mn | Al | Si | Ni | As | Zn | Sb | Bi | P |
| М574х | 76,60 | 0,24 | 0,29 |  | 2,28 |  |  | 0,056 | rem. | 0,018 | 0,0074 | 0,014 |
| М703х | 74,50 | 0,081 | 0,093 | 0,40 | 1,84 | 0,41 | 2,45 |  | 20,06 | 0,0054 | 0,0051 | 0,0078 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Pb | Fe | Mn | Al | Sn | Ni | Zn | Sb | Bi | P |
| М164х | 55,62 | 0,206 | 0,96 | 1,82 | 0,52 | 0,27 |  | [40,5]* | [0,0043] | [0,002] | 0,016 |
| М1184х | 55,30 | 0,22 | 1,16 | 1,65 | [0,56] | 0,30 |  | rem. | 0,0035 | [0,001] | 0,094 |
| М222х | 58,85 | 0,14 | 1,08 | 2,74 | 2,16 | 0,72 | 1,57 | [32,8] | [0,0044] | [0,0025] | [0,01] |
| М1316х | 56,83 | 0,251 | 0,97 | 2,90 | 1,08 |  |  | rem. | 0,0065 | 0,0027 | 0,0117 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Pb | Fe | Sn | Si | Ni | As | Zn | Sb | Bi | P |
| М392х | 60,28 | 0,27 | 0,204 | 0,240 | 0,36 | 0,130 | 0,0039 | 38,36 | 0,0081 | 0,0027 | [0,022] |
| М393х | 63,74 | 0,173 | 0,107 | 0,47 | 0,26 | [0,22] | 0,0075 | [34,87] | 0,0071 | 0,0020 | 0,015 |
| М395х | 71,97 | 0,041 | 0,050 | 2,04 | 0,052 | 0,50 | 0,020 | rem. | [0,002] | 0,00075 | 0,0059 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Pb | Fe | Sn | Si | Ni | As | Zn | Sb | Bi | P |
| М424х | 90,17 | 0,0221 | 0,078 | 0,451 | 0,189 | 0,060 |  | [8,98] | 0,0044 | [0,0024] | [0,020] |
| М1122х | 67,92 | 0,060 | 0,148 | 0,95 |  |  | 0,029 | rem. | 0,0058 | 0,0036 | 0,0033 |

Brass (Chippings 0,2 – 0,5mm, 0,3 – 0,8mm)

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Pb | Fe | Al | Sn | Si | Ni | Zn | Sb | P |
| М636х | 74,39 | 3,01 | 0,058 | [0,007] * |  | 0,0058 |  | 22,45 | 0,0068 | [0,0005] |
| М976х | 64,78 | 1,90 | 0,152 | [0,089] | 0,097 | [0,024] | 0,240 | rem. | 0,0042 | 0,015 |
| М977х | [62,8] | 2,54 | 0,027 | 0,052 | 0,052 | [0,026] | 0,112 | rem. | 0,011 | [0,0064] |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Pb | Fe | Mn | Al | Sn | Si | Ni | Zn | Sb | Bi | P |
| М967х | 60,05 | 1,34 | 0,158 |  | 0,062 | 0,058 | [0,040] | 0,078 | rem. | 0,0052 |  | 0,0213 |
| М1363х | 59,20 | 0,79 | 0,216 | 0,205 |  | 0,200 | 0,203 | 0,080 | 38,48 | 0,015 | 0,0052 | 0,015 |
| М1364х | 60,51 | 1,53 | 0,080 | 0,059 |  | 0,102 | 0,053 | 0,068 | 37,41 | 0,0093 | 0,0085 | 0,021 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Pb | Fe | Mn | Al | Sn | Ni | Zn | Sb | Bi | P |
| М235х | 59,75 | 0,85 | 1,14 | 0,95 | 0,37 | 0,29 | 2,01 | [34,5] | [0,026] | [0,0033] | [0,037] |
| М1183х | [61,75] | 0,33 | 1,33 | 0,57 | 1,14 | 0,66 |  | rem. | 0,0063 | [0,001] | 0,097 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Pb | Fe | Mn | Si | Ni | Zn | Sb | Bi | P |
| М1076х | 64,43 | 0,0154 | [0,15] | 0,027 | [0,004] | [5,25] | rem. | 0,0031 | 0,0049 | 0,0046 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Pb | Fe | Mn | Al | Sn | Si | Zn | Sb | Bi | P |
| М1246х | 78,27 | 0,105 | 0,69 | 0,53 | (0,40) | 0,22 | 3,08 | 16,74 | 0,049 | 0,0056 | 0,024 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Al | Fe | Mn | Si | Sn | Pb | Zn | Sb | P | Ni | Bi | As |
| М223х | 57,14 | [1,36] | 0,81 | 2,40 |  | 0,60 | 0,69 | 35,8 | 0,092 | [0,007] | 1,11 | [0,002] |  |
| М1306х | 54,42 | 0,63 | 0,69 | [4,02] | 0,115 | (0,50) | [0,59] | rem. | 0,095 | (0,031) | 0,57 | 0,019 | 0,056 |

Brass (Chippings 0,2 – 0,5mm, 0,3 – 0,8mm)

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Al | Fe | Mn | Si | Sn | Pb | Zn | Sb | P | Ni | Bi |
| М233х | 60,58 | 1,09 | 0,72 | 2,33 |  | 0,93 | 2,05 | [31,7]* | (0,031) | 0,020 | 0,42 | [0,0052] |
| М1733х | 59,55 | 0,58 | 0,62 | 2,31 | 0,47 | 0,41 | 1,72 | 33,34 | [0,081] | 0,096 | 1,13 |  |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Al | Fe | Mn | Si | Sn | Pb | Zn | Sb | Ni |
| М583х | 65,66 | 1,91 | 0,57 | 0,38 |  | 1,18 | 1,21 | rem. | 0,083 |  |
| М916х | [65,3] | 6,02 | 2,88 | 1,365 | (0,095) | 1,05 | [1,04] | rem. | 0,108 | 0,125 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Al | Fe | Mn | Si | Sn | Pb | Zn | Sb | Ni |
| М896х | (78,58) | 0,199 | 0,280 | 0,83 | (3,31) | 0,33 | (2,73) | rem. | [0,12] | 0,317 |
| М1713х | 68,60 | 0,47 | 0,93 | 0,59 | 0,35 | 1,01 | 2,11 | rem. | 0,080 | 0,93 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Pb | Fe | Sn | As | Zn | Sb | Bi | P |
| А2961х (М204х) | 66,99 | 0,088 | 0,093 | 0,0052 | 0,062 | 32,6 | 0,0050 | 0,0024 | [0,005] |
| А5387х (М378х) | 84,54 | 0,031 | 0,096 |  |  | 15,30 | 0,0057 | 0,0020 | 0,0019 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Pb | Fe | Ni | Sn | As | Zn | Sb | Bi | P |
| А82х | 69,71 | 0,092 | 0,091 |  | 1,05 | 0,060 | rem. | 0,0075 | 0,0018 | 0,0081 |
| А3542х (М45х) | 68,75 | 0,066 | 0,095 | 0,198 | 1,30 |  | [29,4] | 0,0054 | 0,0023 | 0,0072 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Pb | Fe | Mn | Al | Sn | Si | Ni | Zn | Sb | Bi | P |
| А662х | 74,11 | 0,031 | 0,063 | 0,17 | 1,95 |  | 0,65 | 1,96 | rem. | [0,0025] | [0,0005] | 0,0083 |
| А3963х (М163х) | 59,36 | 0,33 | 1,08 | 0,63 | 0,92 | 0,58 |  |  | 36,9 | 0,0063 | [0,003] | 0,0096 |

Brass (Chippings 0,2 – 0,5mm, 0,3 – 0,8mm)

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Pb | Fe | Al | Sn | Si | Ni | Zn | Sb | Bi | P |
| А3543х (М160х) | 73,91 | 2,42 | 0,162 | [0,12]* | [0,25] | 0,075 | 0,461 | 22,4 | 0,0034 | 0,0020 | 0,0037 |
| А3544х (М157х) | 63,60 | 2,87 | 0,128 | [0,28] | 0,226 | 0,338 | 0,448 | 31,8 | 0,0026 | 0,0028 | 0,0080 |
| А3546х (М152х) | 60,75 | 1,054 | 0,086 | [0,37] | 0,138 | 0,203 | 0,237 | 36,8 | 0,0072 | 0,0027 | 0,0088 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Al | Fe | Mn | Si | Sn | Pb | Zn | Sb | Ni |
| А4634х (М1644х) | 57,51 | 0,45 | 0,69 | 0,13 | 0,33 | 0,33 | 0,72 | rem. | 0,081 | 0,99 |
| А6663х (М1643х) | 59,37 | 0,25 | 0,51 | 0,206 | 0,080 | 0,56 | 1,74 | 37,48 | 0,056 | 0,50 |

Brass (Chippings 0,2 – 0,5mm)

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Pb | Fe | Mn | Al | Sn | Si | Ni | Zn | Sb | Bi | P |
| М234х | 61,83 | 1,19 | 1,00 | 1,97 | [0,82] | 0,54 |  | 1,44 | [31,4] | 0,053 | [0,0085] | (0,030) |
| М1006х | 58,95 | 0,143 | 1,08 | 2,94 | 2,27 | 0,70 | (0,036) | 1,60 | 32,25 | 0,0052 |  |  |
| М1663х | 71,39 | 0,84 | 1,57 | [7,13] | 5,24 | 0,073 | 1,79 | 0,071 | rem. | 0,0038 | 0,0037 |  |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Pb | Fe | Mn | Al | Si | Ni | Zn | Sb | Bi | P | Co |
| М516х | 51,12 | 0,099 | 0,152 | 0,26 |  | 0,20 | 11,69 | rem. | 0,0053 | 0,0026 | 0,0091 | [0,13] |
| М517х | 52,00 | 0,13 | 0,219 | 0,43 |  | 0,39 | 12,50 | rem. | 0,0066 | 0,0034 | 0,0101 | [0,2] |
| М1096х | 59,85 | 0,14 | 0,141 | 4,37 | 0,016 | 0,061 | 8,56 | rem. | 0,0057 |  | 0,0131 |  |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Pb | Fe | Mn | Al | Si | Ni | Zn | Sb | Bi | P |
| М906х | (58,19) | 0,66 | 0,104 | [2,04] | 0,78 | 0,80 | (0,14) | rem. | 0,0124 | <0,001 | 0,0077 |
| М1084х | 59,72 | 0,050 | 0,202 | 2,94 | 1,69 | 1,27 | 0,123 | rem. | 0,0075 |  | 0,0105 |

Brass (Chippings 0,2 – 0,5mm)

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Pb | Fe | Mn | Al | Si | Ni | Zn | Sb | Bi | P | B |
| М1066х | 55,93 | 0,73 | 0,52 | 0,70 | 0,111 | 0,050 | 0,132 | 41,62 | 0,0055 | 0,0032 | 0,0123 |  |
| М1163х | 62,61 | 0,109 | 0,52 | 0,75 | 0,0025 | 0,030 |  | rem. | 0,0078 |  | [0,1] | <0,005 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Pb | Fe | Al | Sn | Si | Ni | Zn | Sb | Bi | P |
| М473х | 74,22 | [0,034] | 0,054 |  | 0,0025 | 0,46 |  | 25,09 | 0,0024 | 0,0022 | 0,010 |
| М786х | 64,41 | 2,99 | 0,046 | [0,008] | 0,023 | 1,47 |  | rem. | 0,042 |  | 0,0208 |
| М1426х | 79,37 | 0,052 | 0,021 | 1,89 |  | 0,74 | [5,38] | rem. | 0,0050 | 0,0035 | 0,012 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Pb | Fe | Al | Zn | Sb | Bi | P | S |
| М506х | 83,62 | [0,0040] | 0,078 | 0,43 | 15,72 | 0,0050 | 0,0016 |  |  |
| М1146х | (92,3) | 0,0345 | 0,025 | 0,57 | 6,43 | 0,0060 | 0,0025 | (0,62) | <0,001 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Pb | Fe | Al | Sn | Si | Ni | Zn | Sb |
| М606х | (58,62) | (2,14) | 0,41 | 0,82 | 0,589 | 0,091 | 0,380 | rem. | 0,074 |
| М1696х | 59,01 | 2,31 | 0,51 | 0,251 | 1,02 | 0,225 | 0,53 | rem. | 0,0408 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Pb | Fe | Mn | Al | Sn | Ni | Zn | Sb | P |
| А1453х | 45,23 | 0,084 | 0,83 | 9,60 | 0,53 | 0,29 | 3,48 | rem. | 0,0078 | 0,014 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Pb | Fe | Mn | Al | Si | Ni | Zn | Sb | Bi | Cr | Nb | Zr |
| А3671х | 61,2 | 0,025 | 0,069 | 4,95 | 0,042 | 0,38 | [0,08]* | 32,5 | 0,0070 | 0,0036 | [0,0020] | [0,021] | <0,001 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Pb | Fe | Mn | Al | Si | Ni | Ca | Zn | Sb | Bi |
| А3923х | 60,77 | 1,66 | 0,51 | [2,1] | 0,24 | 1,54 | 0,60 | [0,001] | 32,37 | 0,018 | 0,0032 |

##### Various Copper Alloys (Chippings 0,2 – 0,5mm, 0,3 – 0,8 мм)

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Si | Zn | Pb | Fe | Bi | P | Sb |
| М1576х | 63,24 | 0,30 | 36,08 | 0,089 | 0,103 | 0,0032 | 0,015 | 0,0072 |

IRON BASE

Ore Cu/Fe/V (Chippings 0,2 – 0,5mm)

| RM | Composition, % (by weight) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Fe | SiO2 | V2O5 | P2O5 | As |
| А1571х | 0,56 | 10,0 | 37 | 0,14 | 2,09 | <0,001 |

##### Iron Base Alloy (Chippings 0,2 – 0,5mm, 0,3 – 0,8mm)

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Si | Ni | Mn | Cu | C | Cr | B | Fe |
| А2081х | 3,58 | 3,04 | 2,98 | 1,83 | 1,73 | 1,90 | 0,39 | rem. |

##### Irons (Chippings 0,2 – 0,5mm, 0,3 – 0,8mm)

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Si | C | Ni | Mn | P | Mo | Cr | Ti | S |
| А3331х | 1,41 | 2,42 | 0,60 | 1,21 | 0,313 | 0,98 | 0,41 | 0,070 | 0,024 |
| А3332х | 1,71 | 2,60 | 0,36 | 0,83 | 0,16 | 0,71 | 0,69 | 0,082 | 0,021 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Si | C | Ni | Mn | P | Mo | Cr | Ti | S |
| А3333х | 1,99 | 3,11 | 0,29 | 1,69 | 0,41 | 0,56 | 1,02 | 0,10 | 0,023 |
| А3334х | 2,40 | 3,50 | 0,77 | 0,38 | 0,43 | 0,44 | 1,48 | 0,11 | 0,029 |

MANGANESE BASE

Manganese Base Alloys (Chippings 0,2 – 0,5mm)

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Al | Mo | V | Ni | Pb | Zn | Fe | Sn | Si | Mn | Cu |
| А1881х | 5,31 | 0,87 | 1,15 | 0,21 | 0,10 | 5,82 | 3,60 | 0,31 | 0,47 | 39,6 | [43,2]* |
| А1882х | 0,52 | 0,54 | 0,081 | 1,16 | 0,045 | 0,46 | 2,26 | 0,011 | 0,12 | 41,9 | [53,8] |
| А1883х | 0,051 | 0,019 | 0,23 | 3,43 | 0,082 | 0,93 | 0,73 | [0,10] | [0,10] | 44,4 | [49,9] |
| А1884х | 0,33 | 0,19 | 0,70 | 1,39 | 0,060 | 5,57 | 0,92 | 0,31 | 0,094 | 54,1 | [36,4] |
| А1885х | 1,67 | 0,35 | 0,77 | 2,59 | 0,042 | 2,31 | 1,60 | 0,13 | 0,13 | 55,4 | [35,8] |
| А1886х | 0,65 | 0,58 | 0,023 | 2,98 | 0,021 | 4,55 | 2,64 | 0,015 | 0,061 | 64,7 | [24,0] |
| А1887х | 0,34 | 0,20 | 0,53 | 3,95 | 0,026 | 0,68 | 0,84 | 0,030 | 0,097 | 71,1 | [23,2] |
| А1888х | 0,91 | 0,10 | 0,14 | 1,82 | 0,051 | 0,16 | 0,57 | 0,042 | 0,047 | 72,0 | [25,1] |
| А1889х | 1,47 | 0,40 | 0,27 | 0,85 | 0,044 | 0,29 | 1,01 | 0,11 | 0,053 | 77,7 | [19,2] |

LEAD BASE

Lead Base Alloys (Chippings 0,2 – 0,5mm)

| RM | Composition, % (by weight) |  |
| --- | --- | --- |
|  | Sn | Pb |
| А713х | 9,62 | rem. |
| А714х | 19,41 | rem. |

ZINC BASE

Zinc Base Alloys (Chippings 0,2 – 0,5mm, 0,3 – 0,8mm)

| CRM | Composition, % (by weight) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Zn | Pb | Cd | Fe | Cu | Sn |
| М556х | rem. | 0,88 | 0,195 | 0,122 | 0,036 | 0,0037 |
| М557х | rem. | 1,69 | 0,248 | 0,171 | 0,073 | 0,0076 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Al | Cu | Mg | Zn | Pb | Cd | Sn | Fe | Si |
| М926х | 3,33 | 0,062 | 0,0392 | rem. | 0,0236 | 0,0037 | 0,0052 | [0,0047]* | [0,0029] |
| М1483х | 3,69 | 2,62 | 0,024 | rem. | 0,024 | 0,0065 | 0,0058 | 0,019 | 0,011 |

| CRM | Composition, % (by weight) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Al | Cu | Mg | Zn | Pb | Fe | Sn | Cd | Si |
| М1603х | 10,38 | 1,39 | 0,049 | rem. | 0,0420 | 0,28 | 0,013 | 0,0150 | 0,099 |
| М1613х | 3,78 | 0,062 | 0,030 | rem. | 0,020 | 0,024 | 0,0030 | 0,0078 | 0,012 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Zn | Pb | Cd | Fe | Cu | Sn | As |
| А4171х (М453х) | rem. | 0,011 | 0,0032 | 0,0046 | 0,0040 | 0,0014 | [0,0005] |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Al | Cu | Mg | Zn | Pb | Fe | Sn | Cd | Si |
| А3981х (М283х) | 4,97 | 1,98 | [0,005] | rem. | 0,021 | 0,0039 | 0,0050 | 0,0086 | [0,004] |
| А3984х (М282х) | 9,30 | 2,117 | 0,052 | rem. | 0,043 | 0,0050 | [0,025] | 0,0169 | [0,004] |

| RM | Composition, % (by weight) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Zn | Pb | Al | Fe | Mg | Cu | Cd |
| А4493х (М936х) | rem. | 0,0113 | 0,201 | 0,0036 | 0,0119 | 0,0043 | 0,0041 |

Zinc Base Alloys (Chippings 0,2 – 0,5mm)

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Zn | Pb | Al | Fe | Cu | Sb | Cd |
| А951х | 0,0013 | rem. | 0,009 | 0,047 | 0,0056 | 0,0033 | 0,0020 | 0,0041 |
| А952х | 0,0035 | rem. | 0,020 | 0,061 | 0,013 | 0,0057 | 0,0041 | 0,0053 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Zn | Pb | Al | Fe | Cu | Sb | Cd |
| А953х | 0,0042 | rem. | 0,018 | 0,11 | 0,023 | 0,0096 | 0,0078 | 0,0078 |
| А954х | 0,0065 | rem. | 0,026 | 0,16 | 0,012 | 0,012 | 0,010 | 0,013 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Zn | Pb | Al | Fe | Cu | Sb | Cd |
| А955х | 0,020 | rem. | 0,042 | 0,21 | 0,020 | 0,026 | 0,020 | 0,0032 |
| А956х | 0,0011 | rem. | 0,062 | 0,27 | 0,014 | 0,032 | 0,011 | 0,019 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Zn | Pb | Al | Fe | Cu | Sb | Cd |
| А957х | 0,032 | rem. | 0,086 | 0,39 | 0,082 | 0,058 | 0,034 | 0,034 |
| А958х | 0,048 | rem. | 0,14 | 0,56 | 0,12 | 0,080 | 0,073 | 0,046 |

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Zn | Pb | Al | Fe | Mg | Cu | Si | Cd | Ti |
| А2851х | 0,034 | rem. | 0,020 | 24,08 | 0,054 | 0,011 | 1,68 | 0,18 | 0,0085 | 0,027 |
| А2852х | 0,016 | rem. | 0,021 | 24,17 | 0,096 | 0,024 | 1,08 | 0,11 | 0,0081 | 0,013 |
| А2853х | 0,012 | rem. | 0,023 | 25,83 | 0,167 | 0,050 | 1,02 | 0,075 | 0,0089 | 0,010 |
| А2854х | 0,011 | rem. | 0,035 | 26,32 | 0,13 | 0,075 | 0,49 | [0,07]* | 0,012 | 0,0066 |
| А2855х | 0,0076 | rem. | 0,046 | 27,32 | 0,193 | 0,120 | 0,31 | 0,042 | 0,029 | 0,0042 |
| А2856х | 0,011 | rem. | 0,026 | 28,24 | 0,183 | 0,087 | 1,02 | 0,062 | 0,013 | 0,013 |

Zinc Base Alloys (Chippings 0,2 – 0,5mm)

| RM | Composition, % (by weight) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Zn | Pb | Al | Fe | Mg | Cu | Si | Cd |
| А2921х | 0,0071 | rem. | 0,023 | 7,07 | 0,011 | 0,013 | 1,47 | 0,32 | 0,0092 |
| А2922х | 0,0052 | rem. | 0,012 | 7,57 | 0,0065 | 0,032 | 1,04 | 0,13 | 0,0069 |
| А2923х | 0,0031 | rem. | 0,0081 | 8,24 | 0,0054 | 0,050 | 0,76 | 0,082 | 0,0033 |
| А2924х | [0,0007] * | rem. | 0,0057 | 8,90 | 0,0031 | 0,077 | 0,45 | 0,060 | 0,0014 |

# PURE METALLS

Al 99,999+

| Composition, % (by ppm) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Alloying component and impurity |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Basis |
| Na | Mg | K | Ti | Fe | Co | Ni | Cu | Zn | Sn | Ca | Cr | Mn | Si | Pb | Li | Ga | Al, % |
| <0,01 | 0,08 | 0,07 | <0,01 | <0,05 | <0,03 | <0,05 | 0,1 | <0,05 | <0,05 | 0,03 | <0,01 | 0,07 | <0,1 | <0,1 | <0,001 | <0,1 | 99,999+ |

АL 99,99

| Composition, % (by weight) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Alloying component and impurity |  |  |  |  |  | Basis |
| Fe | Zn | Cu | Ti | Si | Прочие | Al |
| 0,003 | 0,003 | 0,003 | 0,002 | 0,003 | 0,001 | 99,99 |

Bi 98,0

| Composition, % (by weight) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Alloying component and impurity |  |  |  |  |  |  |  | Basis |
| Fe | Cu | As | Te | Pb | Sb | Zn | Ag | Bi |
| 1х10-3 | 1х10-2 | 2х10-4 | 1х10-4 | 1,8 | 5х10-3 | 3х10-3 | 1,2х10-1 | 98,0 |

Kd 99,95

| Composition, % (by weight) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Alloying component and impurity |  |  |  |  |  | Basis |
| Fe | Zn | Cu | Ti | Ni | Pb | Cd |
| 0,002 | 0,004 | 0,01 | 0,005 | 0,002 | 0,02 | 99,95 |

Ko 99,30

| Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Alloying component and impurity |  |  |  |  |  |  |  |  |  |  |  |  |  | Basis |
| Fe | Zn | S | As | Bi | Sb | Sn | Cu | Pb | C | Cd | Ni | P | Mn | Co |
| 0,2 | 0,003 | 0,004 | 0,002 | 0,0005 | 0,001 | 0,001 | 0,03 | 0,0005 | 0,02 | 0,001 | 0,3 | 0,003 | 0,07 | 99,30 |

Cu 99,97

| Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Alloying component and impurity |  |  |  |  |  |  |  |  |  |  |  | Basis |
| Fe | Zn | S | As | Bi | Sb | Ag | Ni | Pb | Sn | O2 | P | Cu |
| 0,004 | 0,003 | 0,003 | 0,002 | 0,001 | 0,002 | 0,003 | 0,002 | 0,003 | 0,002 | 0,001 | 0,002 | 99,97 |

Mg 99,96

| Composition, % (by weight) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Alloying component and impurity |  |  |  |  |  |  | Basis |
| Fe | Mn | Si | Al | Ni | Cr | Cu | Mg |
| 0,004 | 0,004 | 0,005 | 0,006 | 0,002 | 0,003 | 0,002 | 99,96 |

Ni 99,99

| Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Alloying component and impurity |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Basis |
| Fe | Zn | S | As | Bi | Sb | Al | Cu | Pb | C | Mg | Si | P | Mn | Cd | Sn | Ni |  |
| 0,002 | 0,0005 | 0,001 | 0,0005 | 0,0003 | 0,0003 | 0,001 | 0,001 | 0,0003 | 0,005 | 0,001 | 0,001 | 0,001 | 0,001 | 0,0003 | 0,0003 | 99,99 |  |

Sn 99,9

| Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Alloying component and impurity |  |  |  |  |  |  |  |  | Basis |
| Fe | Zn | S | As | Bi | Sb | Al | Cu | Pb | Sn |
| 0,009 | 0,002 | 0,008 | 0,01 | 0,015 | 0,015 | 0,002 | 0,01 | 0,04 | 99,90 |

Pb 99,992

| Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Alloying component and impurity |  |  |  |  |  |  |  |  | Basis |
| Fe | Zn | Cu | As | Bi | Sn | Ag | Sb | Mg+ Ca+Na | Pb |
| 0,001 | 0,001 | 5х10-4 | 5х10-4 | 0,004 | 5х10-4 | 3х10-4 | 5х10-4 | 0,002 | 99,992 |

Ti 99,72

| Composition, % (by weight) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Alloying component and impurity |  |  |  |  |  |  | Basis |
| Fe | Si | Ni | C | Cl2 | N2 | O2 | Ti |
| 0,06 | 0,01 | 0,05 | 0,02 | 0,08 | 0,02 | 0,04 | 99,72 |

Cr 99

| Composition, % (by weight) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Alloying component and impurity |  |  |  |  |  |  |  |  |  |  |  |  |  | Basis |
| Fe | Zn | S | As | Bi | Sb | Al | Pb | Co | Sn | N2 | P | Cu | C | Cr |
| 0,5 | 0,006 | 0,02 | 0,01 | 0,0005 | 0,008 | 0,2 | 0,0008 | 0,005 | 0,004 | 0,04 | 0,02 | 0,01 | 0,03 | 99,0 |

Zn 99,99

| Composition, % (by weight) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Alloying component and impurity |  |  |  |  | Basis |
| Fe | Pb | Cu | Cd | Sn | Zn |
| 0,002 | 0,004 | 0,001 | 0,002 | 0,001 | 99,99 |

Zr 99,93

| Composition, % (by weight) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Alloying component and impurity |  |  |  |  |  |  | Basis |
| Fe | Mo | S | C | P | Cr | V | Zr |
| 0,005 | 0,003 | 0,003 | 0,003 | 0,003 | 0,003 | 0,002 | 99,93 |

Sb 99,9

| Composition, % (by weight) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Alloying component and impurity |  |  |  |  |  |  |  |  | Basis |
| Fe | Zn | S | As | Bi | Sn | Au | Ni | Pb | Sb |
| 0,01 | 0,005 | 0,01 | 0,01 | 0,004 | 0,02 | 6х10-4 | 0,008 | 0,03 | 99,9 |

Mn 99,9

| Composition, % (by weight) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Alloying component and impurity |  |  |  |  |  |  | Basis |
| C | S | P | Fe | Cr | Mo | V | Mn |
| 0,02 | 0,01 | 0,01 | 0,01 | 0,005 | 0,003 | 0,002 | 99,9 |

* Concentration values stated within brackets () are not certified and are listed for information only.

* Concentration values stated within brackets () or [ ] are not certified and are listed for information only.

* Concentration values stated within brackets () or [ ] are not certified and are listed for information only.

* Concentration values stated within brackets () or [ ] are not certified and are listed for information only.

* Concentration values stated within brackets () or [ ] are not certified and are listed for information only.

* Concentration values stated within brackets () or [ ] are not certified and are listed for information only.

* Concentration values stated within brackets () or [ ] are not certified and are listed for information only

* Concentration values stated within brackets () or [ ] are not certified and are listed for information only

* Concentration values stated within brackets () or [ ] are not certified and are listed for information only

* Concentration values stated within brackets () or [ ] are not certified and are listed for information only.

* Concentration values stated within brackets () or [ ] are not certified and are listed for information only.

* Concentration values stated within brackets () or [ ] are not certified and are listed for information only.

* Concentration values stated within brackets () or [ ] are not certified and are listed for information only.

* Concentration values stated within brackets () or [ ] are not certified and are listed for information only.

* Concentration values stated within brackets () or [ ] are not certified and are listed for information only.

* Concentration values stated within brackets () or [ ] are not certified and are listed for information only.

* Concentration values stated within brackets () or [ ] are not certified and are listed for information only.

* Concentration values stated within brackets () or [ ] are not certified and are listed for information only.

* Concentration values stated within brackets () or [ ] are not certified and are listed for information only.

* Concentration values stated within brackets () or [ ] are not certified and are listed for information only.

* Concentration values stated within brackets () or [ ] are not certified and are listed for information only.

* Concentration values stated within brackets () or [ ] are not certified and are listed for information only.

* Concentration values stated within brackets () or [ ] are not certified and are listed for information only.

* Concentration values stated within brackets () or [ ] are not certified and are listed for information only.

* Concentration values stated within brackets () or [ ] are not certified and are listed for information only.

* Concentration values stated within brackets () or [ ] are not certified and are listed for information only

* Concentration values stated within brackets () or [ ] are not certified and are listed for information only.

* Concentration values stated within brackets () or [ ] are not certified and are listed for information only.

* Concentration values stated within brackets () or [ ] are not certified and are listed for information only

* Concentration values stated within brackets () or [ ] are not certified and are listed for information only.

* Concentration values stated within brackets () or [ ] are not certified and are listed for information only.

* Concentration values stated within brackets () or [ ] are not certified and are listed for information only..

* Concentration values stated within brackets () or [ ] are not certified and are listed for information only..

* Concentration values stated within brackets () or [ ] are not certified and are listed for information only..

* Concentration values stated within brackets () or [ ] are not certified and are listed for information only..